Colorado Rose Red Granite

Specification sheet

SPG						2.655

Absorption					.20

Solid Weight					175 lb/cuft

Corroded Weight				89 lb/cuft

LA Abrasion					27%

Crushing Strength				28,000 psi

Colorado Rose Red Inc. 148 Cheyenne Ct Lyons CO 80540 P: 3037473718 F:3033626353